F10 Natural Stone Walling Bricks

HERITAGE PORTLAND STONE® BRICKS

Natural stone bricks to BS EN 771-6: For compliance with the Construction Products Regulations, a current UKCA/CE Certificate and Declaration of Performance is available from Albion Stone. All declared values are based on extensive testing and approved by a company director.

Dimensional Tolerances: D2 Tolerance, Range R2 (as per BS EN 771-6)
Configuration: Solid unit (no frog)
Apparent Density: 2190 kg/m³ (BS EN 1936)
Compressive Strength: Average 47.97 MPa / LEV 37 MPa (BS EN 1926)
Water Absorption: 5.85% (BS EN 13755)
Durability: Category F2 (suitable for freeze/thaw exposure)
Soluble Salts: None detected
Reaction to Fire: Class A1
Sustainability Declaration: Verified EPD – 44.7 kgCO₂/tonne (A1–A3)

Face dimensions: 215mm x 102.5mm x 65mm
Dry Weight per Brick: Approx. 3.1kg
Pack Size: 300 bricks per pallet

Petrographic Name (BS EN 12407): Jurassic Limestone, Portland Stone
Denomination (BS EN 12440): Heritage Portland Stone
Colour: Pale cream / off-white
Origin: Jordans Mine, Portland, Dorset, UK

Finish: Supplied with a clean sawn finish. Range panels are available for review at Albion Stone’s Portland mine and will act as control samples for projects.

Supplier:
Albion Stone Plc
Easton Street, Portland, Dorset DT5 1BW
Tel: +44 (0)1737 771772
www.albionstone.com

Quality Assurance:
Quality Management: ISO 9001
Environmental Management: ISO 14001
Responsible Sourcing: BES 6001 (Excellent)