**F10 Natural Stone Walling Bricks**

**HERITAGE PORTLAND STONE® BRICKS**

Natural stone bricks to BS EN 771-6: For compliance with the Construction Products Regulations, a current UKCA/CE Certificate and Declaration of Performance is available from Albion Stone. All declared values are based on extensive testing and approved by a company director.

**Dimensional Tolerances:** D2 Tolerance, Range R2 (as per BS EN 771-6)  
**Configuration:** Solid unit (no frog)  
**Apparent Density:** 2190 kg/m³ (BS EN 1936)  
**Compressive Strength:** Average 47.97 MPa / LEV 37 MPa (BS EN 1926)  
**Water Absorption:** 5.85% (BS EN 13755)  
**Durability:** Category F2 (suitable for freeze/thaw exposure)  
**Soluble Salts:** None detected  
**Reaction to Fire:** Class A1  
**Sustainability Declaration:** Verified EPD – 44.7 kgCO₂/tonne (A1–A3)

**Face dimensions:** 215mm x 102.5mm x 65mm  
**Dry Weight per Brick:** Approx. 3.1kg  
**Pack Size:** 400 bricks per pallet

**Petrographic Name (BS EN 12407):** Jurassic Limestone, Portland Stone  
**Denomination (BS EN 12440):** Heritage Portland Stone  
**Colour:** Pale cream / off-white  
**Origin:** Jordans Mine, Portland, Dorset, UK

**Finish:** Supplied with a clean sawn finish. Range panels are available for review at Albion Stone’s Portland mine and will act as control samples for projects.

**Supplier:**  
Albion Stone Plc  
Easton Street, Portland, Dorset DT5 1BW  
Tel: +44 (0)1737 771772  
[www.albionstone.com](https://www.albionstone.com)

**Quality Assurance:**  
Quality Management: ISO 9001  
Environmental Management: ISO 14001  
Responsible Sourcing: BES 6001 (Excellent)